## Slide 1
Molecular Nanographene as Quantum Units
Fanmiao Kong
21/06/2022

## Slide 2
“Cutting”
Magnetic Zigzag Edge States in Graphene Nanoribbon
Gapless
1D zigzag graphene nanoribbon
2D graphene
Band gap
Spin-polarized zigzag edge states
Spin up
Spin down
1
Band structure
Band structure

## Slide 3
Magnetic Zigzag Edge States in Graphene Nanoribbon
P Useful for spintronic devices
P Predicted to have long spin coherence time
P. Ruffieux et al., Nature 531, 489 (2016)
J. Fischer, B. Trauzettel, D. Loss, Physical Review B 80, 155401 (2009).
O Synthesized in high vacuum. Chemically unstable
O Difficult to study the spin states
2

## Slide 4
Zigzag Edge in Nanographene Molecule
1D zigzag graphene nanoribbon
0D nanographene molecule
3
Notes: Further decrease the dimension.
Instead of study the extended structure, we study the small molecule, which still have a zigzag element

## Slide 5
Zigzag Edge in Nanographene Molecule
1D zigzag graphene nanoribbon
0D nanographene molecule
Synthesized by Jishan Wu’s group at NUS
Y. Ni et al., Angewandte Chemie 130, 9845-9849 (2018)
3
Notes: Further decrease the dimension.
Instead of study the extended structure, we study the small molecule, which still have a zigzag element

## Slide 6
Zigzag Edge in Nanographene Molecule
Bulky group to enhance stability and solubility
Peri-tetracene
Synthesized by Jishan Wu’s group at NUS
Y. Ni et al., Angewandte Chemie 130, 9845-9849 (2018)
3

## Slide 7
Zigzag Edge in Nanographene Molecule
Bulky group to enhance stability and solubility
Peri-tetracene
Synthesized by Jishan Wu’s group at NUS
Y. Ni et al., Angewandte Chemie 130, 9845-9849 (2018)
3
Does zigzag edge spin state still exist?

## Slide 8
Peri-tetracene
Clar’s sextet rule:
More aromatic rings
 More stable
52.5% diradical character
Y. Ni et al., Angewandte Chemie 130, 9845-9849 (2018)
Peri-tetracene
4

## Slide 9
Peri-tetracene
52.5% diradical character
Y. Ni et al., Angewandte Chemie 130, 9845-9849 (2018)
Peri-tetracene
108.4 meV
Thermally accessible
4
singlet
triplet
Clar’s sextet rule:
More aromatic rings
 More stable

## Slide 10
Peri-tetracene
Spin density of triplet state
Spin up
Spin down
5

## Slide 11
Zigzag Edge in Extended Structures
6
Notes: They all have edge states around Fermi level. Some can be spin-polarized
No Dirac cone, not even 1D band structure, but the spin-polarized zigzag edge states are preserved in this small molecule

## Slide 12
Zigzag Edge in Extended Structures
Local Density of States (LDOS) calculated by tight binding model
Spin-polarized states in zigzag edge
6
Notes: They all have edge states around Fermi level. Some can be spin-polarized
No Dirac cone, not even 1D band structure, but the spin-polarized zigzag edge states are preserved in this small molecule

## Slide 13
Zigzag Edge in Extended Structures
Local Density of States (LDOS) calculated by tight binding model
Spin-polarized states in zigzag edge
6
Topological phase
Quantum spin chain
Notes: They all have edge states around Fermi level. Some can be spin-polarized
No Dirac cone, not even 1D band structure, but the spin-polarized zigzag edge states are preserved in this small molecule

## Slide 14
CW EPR Spectrum of Peri-tetracene
CW EPR:
Continuous Wave Electron Paramagnetic Resonance
S = 0
S = 1
mS = +1
mS = 0
mS = +1
Magnetic field
Energy
Microwave
7

## Slide 15
CW EPR Spectrum of Peri-tetracene
CW EPR:
Continuous Wave Electron Paramagnetic Resonance
S = 0
S = 1
mS = +1
mS = 0
mS = +1
Magnetic field
Energy
Microwave
7

## Slide 16
CW EPR Spectrum of Peri-tetracene
CW EPR:
Continuous Wave Electron Paramagnetic Resonance
Hamiltonian to describe the system:
Zeeman energy
Hyperfine interaction
S = 0
S = 1
mS = +1
mS = 0
mS = +1
Magnetic field
Energy
Microwave
7

## Slide 17
Pulsed EPR Study: Spin-Lattice Relaxation
Measure T1 by picket-fence sequence
Pulse delay time
8
Echo intensity

## Slide 18
Pulsed EPR Study: Spin-Lattice Relaxation
9.5 GHz
34 GHz
Measure T1 by picket-fence sequence
Pulse delay time
8
Echo intensity

## Slide 19
Pulsed EPR Study: Spin-Lattice Relaxation
9.5 GHz
34 GHz
Measure T1 by picket-fence sequence
Pulse delay time
vs. is fitted by direct and Raman relaxation processes
8
Echo intensity

## Slide 20
Pulsed EPR Study: Spin-Lattice Relaxation
9.5 GHz
34 GHz
Measure T1 by picket-fence sequence
Pulse delay time
vs. is fitted by direct and Raman relaxation processes
reaches 0.6-15 ms for T > 80 K in dOTP solution
8
Echo intensity

## Slide 21
Spin Coherence
Carr-Purcell-Meiboom-Gill (CPMG) sequence
(: Hahn echo)
9

## Slide 22
Spin Coherence
Echo decay with nuclear modulation effect
Carr-Purcell-Meiboom-Gill (CPMG) sequence
(: Hahn echo)
9

## Slide 23
Spin Coherence
Echo decay with nuclear modulation effect
Fourier transform
Carr-Purcell-Meiboom-Gill (CPMG) sequence
(: Hahn echo)
9
Notes: Fourier transforms reveal frequencies typical of hydrogen (14-15 MHz), deuterium (2.2 MHz), and chlorine (1.3 MHz)
intrinsic hyperfine of the zigzag segment is dominant

## Slide 24
Spin Coherence
Coherence time and fast relaxation time constant from bi-exponential fitting
reaches 100 µs at 80 K in CS2, exceeding theoretical predictions
10
Notes: Here we use the convention: spin memory time

## Slide 25
Spin Coherence
Further increasing coherence time up to 400 µs by dynamical decoupling from the nuclear bath
Coherence time and fast relaxation time constant from bi-exponential fitting
10
reaches 100 µs at 80 K in CS2, exceeding theoretical predictions
Notes: intramolecular vibration modes contribute the most to the relaxation

## Slide 26
Conclusion
Short zigzag segment in molecular nanographene as a gateway to understand extended systems.
Spin coherence time exceeding theoretical predictions.
More possibilities to build extended graphene nanoribbon systems, which can form quantum spin chain or host topological non-trivial phase.
11
Notes: Plenty of room to further optimize

## Slide 27
Acknowledgements
University of Oxford
Lapo Bogani
Federico Lombardi
Michael Slota
Karen Yan
William Myers
NUS
Yong Ni
Jishan Wu
Notes: intramolecular vibration modes contribute the most to the relaxation